## Slide 1: PfQ2 – Virtual
Gregory D. Fuchs
School of Applied & Engineering Physics Cornell University, Ithaca, NY USA
Spin and Orbital Resonance Driven by a Mechanical Resonator
June 23, 2020

## Slide 2: Cornell spin-mechanics: acknowledgements
Fuchs Group (Cornell)
Huiyao Chen*
Raphaël Daveau*
Evan MacQuarrie*
Sunil Bhave Group (Purdue ECE)
Noah Opondo
Alex Jiang
Evan
Huiyao
*group alumni
Raphaël

## Slide 3: Applications of nitrogen-vacancy (NV) centers
Quantitative, atomic-scale probe at room or low temperature
  Magnetometry
  Thermometry
  Electrometry
Quantum information
  Multi-qubit quantum node
  Photonic quantum interface
  Hybrid quantum interface
Image: Qzabre.com
Hansen Group, Delft, 2015
Entanglement between long-lived qubits

## Slide 4: Diamond NV centers: an experimentalist’s introduction
Nitrogen-vacancy (NV) center in diamond
S=1 spin defect in diamond
Model system for spins in the quantum limit
Experimentally simple:
  Solid state
  Address individually or in ensembles
  Optical spin initialization and read-out
  Room temperature quantum coherence
3A
3E
Dark,
spin selective
relaxation
-1
+1
0
-1
+1
0
Orbital
Spin
Optical cycle: initialization and read-out
read “dark”
read “bright”
Photoluminescence image
Review article: Dobrovitski, Fuchs, Falk, Santori, Awschalom, Ann. Rev. CMP (2013)

## Slide 5: Hybrid quantum systems
Color Center
Resonator,
Cavity
Coupling different degrees of freedom
Long coherence lifetime
Sensing
Coherent coupling to photons
Different qubit
Logic
Connectedness
Scaling
Driving
Quantum control

## Slide 6: Coupling to resonators via strain
Both spin and optical transitions couple to strain
Strains that retain symmetry shift eigenstates
Strains that lower symmetry couple/shift states, allow transitions
  Spin:
  Orbital*:
Orbital-strain interaction is ~104× larger than spin-strain
spin
orbital
*These animations are not fully correct for the case of orbital strains, the situation is a little complex, but this is true in spirit.

## Slide 7: Past work: spin-mechanical coupling to spin
t0 (μs)
mI=+1 only
E. R. MacQuarrie, T. A. Gosavi, A. M. Moehle, N. R. Jungwirth, S. A. Bhave, and G. D. Fuchs, Optica 2, 233 (2015)
E. R. MacQuarrie, T. A. Gosavi, N. R. Jungwirth, S. A. Bhave, and G. D. Fuchs, PRL 111, 227602 (2013)
Spectroscopy
E. R. MacQuarrie, T. A. Gosavi, S. A. Bhave, and G. D. Fuchs, PRB 92, 224419 (2015)
See also work by Jayich (UCSB), Awschalom (UChicago), Wang (Oregon), Malentinsky (Basel), Loncar (Harvard), Wrachtrup (Stuttgardt), …
93
95
94
Coherent Control
Decoherence protection
E. R. MacQuarrie, M. Otten, S. K. Gray, and G. D. Fuchs, Nat. Commun. 8, 14358 (2017)
Room-temperature excited-state spin strain interaction

## Slide 8: Outline
1. Engineering the optical transition using orbital-state resonance
2. Engineering stronger spin-phonon coupling by reducing resonator volume
3. Revisiting ground-state spin-strain: the single quantum transition

## Slide 9: Engineering the optical transition with strain at low-T
For at T< 10 K, full orbital manifold is stable: 3E = (2 orbital) × (3 spin) = 6 levels
Consider only ms=0 levels, and static terms for simplicity:
Unperturbed
x and y shift together
Longitudinal Strain
x and y shift apart
Transverse Strain
x and y mix
Shear Strain
See e.g. Doherty et al., NJP 13, 025019 or Lee et al., PR Applied 6, 034005
Optical transition

## Slide 10: High-frequency diamond mechanical resonator
High-overtone bulk-mode acoustic resonator (HBAR)
  Fabery-Perot “type” phonon cavity: diamond surface as acoustic mirrors
  Driven by a piezoelectric transducer (either AlN or ZnO)
  Modes in the range 0.5 – 2 GHz
  Mechanical Q-factor ≈ 400 – 4000 typical
  Generates ≈ 10 - 100 MPa of stress along [001]
diamond

## Slide 11: Dynamic Hamiltonian for NV excited orbital states
In a strongly-driven system, the eigenstates aren’t obvious!
For our geometry in the sideband-resolved limit:

## Slide 12: Driving the orbital states in the side-band resolved limit
“frequency modulation”
“Orbital state mixing”
Δ
Fluorescence
See Golter et al., PRL 2016
Line amplitude )
FM modulation in sideband-resolved limit,
Energy
Avoided-crossing/Rabi coupling; nth term n+1 phonon process
Displaced oscillator transformation see, e.g. Ashab et al. PRA 75, 032301 (2007)

## Slide 13: Photoluminescence excitation spectroscopy
Ex
EY
A2
Scan the frequency of a tunable laser
Measure sideband fluorescence

## Slide 14: Orbital driving: 2
ωm = 1.4 GHz, Ex/Ey splitting = = 10.4 GHz
Bessel function fit shows > 14 GHz (very strongly driven)
Shift apart of Ex, Ey show multi-phonon orbital Rabi coupling
H. Y. Chen, E. R. MacQuarrie, G. D. Fuchs PRL 120, 167401 (2018)
PLE
Photoluminescence Excitation Spectroscopy (PLE)

## Slide 15: Orbital driving: 2
On resonance, 2-phonon driving between
Direct observation of Autler-Towns (or Rabi) splitting
Splitting ~
Small contribution from other phonon orders
H. Y. Chen, E. R. MacQuarrie, G. D. Fuchs PRL 120, 167401 (2018)
Data
Model
3.2 GHz

## Slide 16: So what?
Direct quantum control within the orbital manifold
Orbital dynamical decoupling  toward improved coherent optical transitions for spin-photon interface (quantum network, quantum repeater)
Transverse E-field,
Energy
Notice = 0 on resonance
Insensitive to transverse field fluctuations
Not insensitive to longitudinal (A1-type) field fluctuations

## Slide 17: Outline
1. Engineering the optical transition using orbital-state resonance
2. Engineering stronger spin-phonon coupling by reducing resonator volume
3. Revisiting ground-state spin-strain: the single quantum transition

## Slide 18: From HBAR to Semi-confocal HBAR (COMSOL simulation)
1. Reduce t
2. Reduce λ
3. Reduce f(g)
3x104 times smaller volume
10 times more strain
10 μm
strain
HBAR
Semi-confocal HBAR
10 μm
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters 19, 7021-7027 (2019)
Notes: To make the transition from HBAR to Semi-confocal HBAR.
Here is what we can do to achieve the small mode volume
1. Reduce the thickness of the resonator,
2. Increase the frequency of the resonator,
3. And finally add more confinement by creating a curved focusing boundary, that matches with the wave front of the acoustic beam.
The strain profiles are from the COMSOL simulation with the same voltage drive source, we can tell, not only the semi-confocal HBAR design can confine phonons in a small mode volume <10 um3,
The strain generated by the same drive is also bigger.
....as mentioned earlier, Optically, the curved surface also suppresses the light refraction, making it more efficient to collect fluorescence from the NV centers.

## Slide 19: Device Fabrication
High rate DRIE etch 50 µm diamond (optical graded) down to 10 - 20 µm membrane. (~5 μm/hr)
10 μm
Milling a parabolic curved surface/lens using Focused Ion Beam (FIB);
Backside ZnO piezoelectric transducer fabrication.
10 μm
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters 19, 7021-7027 (2019)
Notes: In terms of fabrication, let me present the process flow with a video.
we start from a DSP single crystal substrate,
the first step is to thin the substrate down to 10um using deep reactive ion etching method;
Then, we use focused ion beam to mill the lens structure on one side of the membrane;
In the end, we put down piezoelectric transducers and antenna on the other side of the membrane, aligned to the previously made lens.
A few images of the made devices are shown on the slides as well.

## Slide 20: Spin Characterization
Polarizes nuclear spins
~3.15 GHz
Spectroscopy
P+1
Acoustically-driven Rabi oscillations
Ramsey fringes in single and double quantum basis
Double-quantum {+1,-1} basis is more sensitive for magnetometry
Direct quantum control can enable new magnetometry sequences
As power efficient as the magnetic antenna!
~100% polarization of 14N nuclear spins
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters 19, 7021-7027 (2019)

## Slide 21: Outline
1. Engineering the optical transition using orbital-state resonance
2. Engineering stronger spin-phonon coupling by reducing resonator volume
3. Revisiting ground-state spin-strain: the single quantum transition

## Slide 22: Spin resonance driven by an ac strain
Transverse B-field couples & or & (single quantum)
  → Conventional magnetic resonance spin control
  → selection rule
Transverse strain couples & (single or double)
  → NV spin controlled by lattice stress/strain
  → selection rule
Bennett et al. PRL 2013 [Theory @ Harvard]
MacQuarrie, … GDF, PRL (2013)
Udvarhelyi et al., PRB 2019 [Theory @Budapest]
Measuring using cantilevers:
Ovartchaiyapong et al., Nat. Comm. (2014) [UCSB]
Teissier et al., PRL (2014) [Basel]
  = 2.3(3) MHz/GPa
  = 4.86(2) MHz/GPa
= ???
(DFT predicts ~0.06b)
P. Udvarhelyi, PR B (2018).

## Slide 23: Decomposing the driving field vectors
Total driving field
The phase of and depend on detuning from the mechanical resonance in a know-able way
The total SQ driving field is
  (on the transducer ) = (at the leads )
  (SQ stress Rabi) = (DQ stress Rabi)
  All depend on the resonator properties
Therefore
  (by comparing Rabi at and at another frequency)
  = is the primary unknown

## Slide 24: Rabi spectroscopy of the transition
fm
fm
fe
PL
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).
Notes: We use Rabi spectroscopy to measure magnetic Rabi field at the marked blue cross location on the device.
We first focus on the mechanical mode at fr =3.132 GHz aiming at +1 SQ transition.
In the measurement, we use resonant microwave driving at a fixed power (10dbm), to record the NV spin Rabi oscillation at each frequencies
Using the sequence shown above.
The Fourier transform of the Rabi spectroscopy data (on the bottom) reports the Rabi field amplitude frequency dependence.
Here, we see two resonances that correspond to mechanical and electrical resonances of the device.
Similarly, we perform Rabi spectroscopy on |−1⟩ ↔ |+1⟩ DQ transition to measure acoustic Rabi field Ωσ2(f) at the marked orange cross location in the device.
Here ,we see a single Lorenzian peak showing the mechanical resonance behavior of the device.
Lastly, we we perform SQ Rabi spectroscopy at the same orange cross location. We see complex behavior in the total Rabi field.
because magnetic and acoustic fields jointly act on this transition, and the probed NV center ensemble includes NV centers coupled to both anti-node and node of the acoustic wave, which introduces spatial inhomogeneity in the acoustic field.

## Slide 25: Rabi spectroscopy of the transition
where
How to solve electromechanical phase ?
PL
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).
Notes: We also perform similar measurements on a different acoustic mode at 2.73 GHz to probe the |−1⟩ SQ transition. The results are shown here.
(click)
We now know the amplitude of the Rabi fields,
however, their electrical phase information, theta, is still unknown.
how do we solve this?
it turns out that Theta depends on resonator electromechanical characteristics, and can be inferred from an electrical model of the device.

## Slide 26: Equivalent circuit model
Circuit model fit using modified Butterworth-Van Dyke model
yields electromechanical phase information
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).
Notes: The electromechanical response of a piezoelectric resonator like our device can be modeled using an electrical equivalent circuit known as the modified Butterworth–Van Dyke (mBVD) model shown above.
With magnetic and acoustic field measured experimentally, we can perform model fitting. using the equation given here. The results are shown on the right of the slide.
The fitted circuit model not only reproduces the measured Rabi field amplitude, but also contains the requisite phase information.
(beta, can be experimentally measured by driving the transducer off resonance, and turned out be be around 1.3 in our device.)
We are now ready to tackle alpha and phi.

## Slide 27: Use quantum master equation to simulate an array of ()
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
Structural Similarity Index (SSIM)
Simulation
1.5
Simulation
Data
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).
Notes: To interpret the Rabi spectroscopy result, evaluate α and thus extract the spin stress susceptibility, b′, we implement a quantum master equation simulation for an ensemble of NV centers.
We did simulation for a range of {α,φ} values, and compare them to the experimental data by calculating their structural similarity index.
The heat map on the right shows the result.
Higher SSIM value indicates better match of simulation to experiments.
and We find the best match at circled region, where α is around 0.5, for the 3.13 GHz mode measurement
The corresponding simulated Rabi spectroscopy results are shown below, which agrees well with the experimental observation.

## Slide 28: Use quantum master equation to simulate an array of ()
1.5
Structural Similarity Index (SSIM)
Data
Simulation
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
…
Simulation
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).
Notes: Similar simulation is done for the 2.7 GHz mode and the best match also occurs at , α = 0.5

## Slide 29: Single quantum strain driving: summary of results
, an order-of-magnitude higher than predicted
This opens the door to all-acoustic quantum control over NV centers, NV centers, ensembles.
Interesting for NV-based sensors
  Higher sensitivity for DQ sensing
  Smaller footprint than a magnetic antenna
  Local selective spin control
  More scalable
  Uniform control of NV ensemble in growth layer
  Potentially lower power
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).

## Slide 30: Cornell spin-mechanics: acknowledgements
Fuchs Group
Evan MacQuarrie
Huiyao Chen
Raphael Daveau
Sunil Bhave Group
(Purdue)
Noah Opondo
Alex Jiang
Probing acoustically dressed optical transitions and multi-phonon orbital transitions
H. Y. Chen, E. R. MacQuarrie, and G. D. Fuchs PRL 120, 167401 (2018).
Engineering stronger electron-phonon interactions in high-efficiency diamond acoustic resonators
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters 19, 7021-7027 (2019)
Measuring the acoustically driven single quantum spin transition of NV centers
H. Y. Chen, S. A. Bhave, and G. D. Fuchs, Phys. Rev. Applied 13, 054068 (2020).

## Slide 31: Orbital driving: 2
ωm = 1.4 GHz, Ex/Ey splitting = = 10.4 GHz
Bessel function fit shows > 14 GHz (very strongly driven)
Shift apart of Ex, Ey show multi-phonon orbital Rabi coupling
H. Y. Chen, E. R. MacQuarrie, G. D. Fuchs PRL 120, 167401 (2018)
PLE
Photoluminescence Excitation Spectroscopy (PLE)

## Slide 32: Orbital driving: 2
On resonance, 2-phonon driving between
Direct observation of Autler-Towns (or Rabi) splitting
Splitting ~
Small contribution from other phonon orders
H. Y. Chen, E. R. MacQuarrie, G. D. Fuchs PRL 120, 167401 (2018)
Data
Model
3.2 GHz

## Slide 33: Mechanical resonance of the low temperature orbital states
At low temperature, the optical transition is coherent
  Basis for spin-photon entanglement
Orbital-strain coupling is ~104 × (spin-strain coupling)
  Experimental demonstrations in Santa Barbara (Jayich), Oregon (Wang)
Idea: use coherent orbital resonance to engineer the optical transition

## Slide 34: Dynamic Hamiltonian for NV excited orbital states
In a strongly-driven system, the eigenstates aren’t obvious!
Displaced oscillator basis :
where and
For our geometry in the sideband-resolved limit:
See e.g. Ashab et al. PRA 75, 032301 (2007)
(Alternate description: Landau-Zener-Stückelberg transitions through strain-coupled states)

## Slide 35: Optical Characterization
PL confocal scan (Uniform Ensemble)
X
Y
Z
PL (MHz)
Expect enhanced optical collection
For our device, a factor of ~2.3
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters in press, (2019)

## Slide 36: Diamond NV centers: an experimentalist’s introduction
Nitrogen-vacancy (NV) center in diamond
S=1 spin defect in diamond
Model system for spins in the quantum limit
Experimentally simple:
  Solid state
  Address individually or in ensembles
  Optical spin initialization and read-out
  Room temperature quantum coherence
3A
3E
Dark,
spin selective
relaxation
-1
+1
0
-1
+1
0
Orbital
Spin
Optical cycle: initialization and read-out
read “dark”
read “bright”
Photoluminescence image
Review article: Dobrovitski, Fuchs, Falk, Santori, Awschalom, Ann. Rev. CMP (2013)

## Slide 37
ZnO or AlN
Top electrode
Bottom electrode
Manson Model:
Equivalent circuit model (mBVD):
HBAR: 105 um2
scHBAR: 102 um2
Notes: How do we generate GHz strain waves? we fabricated a diamond HBAR device.
For our experiment we fabricated a diamond high- overtone bulk-mode acoustic resonator (HBAR) device that consists of a zinc oxide piezoelectric transducer patterned on the surface of a type IIa diamond substrate, purchased from Element Six.
We designed the thickness of the piezoelectric layer to accommodate GHz frequency resonance modes.
The electrical response of the HBAR device is shown on the right, which features a range of GHz mechanical resonance modes.
the strain wave enters the diamond (click),
Upon resonant driving the transducer, a longitudinal strain wave enters the acoustic cavity formed by the parallel [100] diamond surfaces.
mechanically driving the NV centers in the bulk. NV centers located at an anti-node of the resulting standing wave experience the strongest strain modulation.
On the opposite diamond face, we also patterned a microwave antenna for conventional magnetic resonance manipulation of the NV center spin.

## Slide 38: Orbital-strain driving and resonance
ωm = 1.4 GHz, Ex/Ey splitting = 10.4 GHz
NV1
Data
Model
ωm = 1.6 GHz, Ex/Ey splitting = 3.2 GHz
Model
Data
NV2
9 orders of coherent Raman sidebands
Direct Autler-Towns (or Rabi) splitting of orbital states
Nonlinear phonon orders
Manipulation of orbital manifold
H. Y. Chen, E. R. MacQuarrie, G. D. Fuchs PRL 120, 167401 (2018)

## Slide 39: Resonator Characterization
Both fab on diamond and 4H-SiC substrate
A factor of 4x enhancement in Q brought by the lens confinement at RT.
SiC substrate, f*Q factor>1013 at 77 K.
Likely extrinsic differences – better quality polish, flatness, etc.
Silicon Carbide
Diamond
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters 19, 7021-7027 (2019)
Notes: On the other hand, we care about the mechanical quality factor of these devices.
We did similar device fabrication on two types of substrate, diamond and Silicon carbide.
In SiC, for a planar structure, without the lens, the quality factor of these devices are around 500. After milling the lens using FIB, we achieved enhancement in the quality factor almost 4 times.
As we cool these devices down to nitrogen temperature, we realized f*Q product >10^13.
In diamond, the results are not as pleasing, limited by the substrate processing technique, we have quality factor ~200.

## Slide 40: Comparison with fundamental limits
Not intrinsically limited
H. Y. Chen, N. F. Opondo, B. Jiang, E. R. MacQuarrie, R. S. Daveau, S. A. Bhave, and G. D. Fuchs, Nano Letters 19, 7021-7027 (2019)