## Slide 1: CNES activities in detectors for scientific space missions
Alain BARDOUX
alain.bardoux@cnes.fr
SDW Florence 2013 – A Bardoux

## Slide 2: CNES : French Space Agency
Corot
Exoplanets
Asterosismology
Gaia
Star mapping
Helios, CSO
Earth obs for Defence
SPOT, Pleiades
Earth onservation
IASI, IASI-NG
Atmospheric
sounding
Herrschel
Stars & Galaxies
evolution
Athena
Black hole
High energy astronomy
B mode
Origin of Univrse
Echo
Exoplanets
Microcarb
CO2 survey
Exomars
Mars Exploration
And many others
SDW Florence 2013 – A Bardoux
Notes: CNES is leading or involved , in a lot of space missions, National, bi /multilatera and in ESA frame
The missions supported by CNES are not limited to those presented here :
Only those requiring detector development are evocated here

## Slide 3: A travel through wavelengths
CCD
CMOS
AlGaN
I-CCD
InGaAs
MCT
a-Si
InSb
QWIP
NbSi
TES
Diamond
CdTe
Tantal
Doped Si
Germanium
DSSD
…. and technologies
SDW Florence 2013 – A Bardoux
Notes: Iwill talk only aboutpre-developments, not on on-going missions
This pesentation will focus only on certain technologies

## Slide 4: X Ray
SDW Florence 2013 – A Bardoux

## Slide 5: Missions In X ray domain
Missions in development
      Taranis
      SVOM
      Solar Orbiter
Mission in pre-development (not decided)
  Athena (black hole matter survey)
  Spectral domain 0.2-6keV (Instrument XMS, résolution 3eV@6keV)
  nominal solution based on TES (Goddard, NIST)
      Développement of an alternative solution
      Loft
      French developemntsfocused on Front end ASIC’s
SDW Florence 2013 – A Bardoux

## Slide 6: Xray microcalorimeter
Detection of Xray photons
Counting
Energy measurement
Split of 3 functions
  Absorbeur High Z
  Sensor
  Thermal insulation
  + Specific electronics
SDW Florence 2013 – A Bardoux

## Slide 7: Xray microcalorimeter : on going development
Main axis
collective manufacturing
improvement of existing Technology (PACS) Silicon compatible technology
Goal
32x32 demonstrateur for Athena
Technological choices
  Absorbeur High Z Tantal
  Sensor Doped Silicon
  Thermal insulation SiO2
  Sensor temperature 50 to 70mK
SDW Florence 2013 – A Bardoux

## Slide 8: Xray microcalorimeter Readout circuit
SDW Florence 2013 – A Bardoux
HEMT
SiGe ASIC
Several stages to optimize thermal budget

## Slide 9: Xray microcalorimeter : performances
Signal :
30 to 100 µV/keV ie 150µV to 600 µV for a 6keV photon
Energy range : 300 ev to 30 keV
Dynamic : 300eV to 30keV ie 9µV to 3mV
Noise
Expected resolution : 6eV FWHM at 6 keV
Noise 0,1µV to 0,3µV
Power dissipation
Goal 128 mW for 4000 pixels
ie 1mW for 32 pixels
SDW Florence 2013 – A Bardoux

## Slide 10: Xray microcalorimeter : realizations
SDW Florence 2013 – A Bardoux
Notes: µcal X (X mlouo jusqu » a keV)
solu abase de TES
brique techno : Asic CL reprise de Asci DCMB (SiGe)
integration en interco : synergie avvec Artemis
portage sur PF 100mm
obj demonstarteur 32x32 pour athena
Irfu adossé au Sedi et leti
On va deytecteer photon X et on faiut compatge en ragardant son energie
Asic de lecture
Reprise de la techno Pacs en la simplifiant (terreau pour IR lointain)
Descente à 50 mK pour ameliorer perfon , aux carac visées
Fab collective : c’est la force leti
Report absorbeuer : dans ces lon d’onde o utilise tanatale
Simplification de setapes techno
PTA : paforme techno amon

## Slide 11: Other activities in Xray domain
LOFT :((IRAP) ultra low noise and consomption front end ASIC (15e ENC, 200µW)
Compton telescop : (APC) : tower of DSSD (souble stripped Si detector) up to 100MeV (See Youri Dolgorouky’s talk)
Germanium stripped detector (IRAP) ultimate performance spectro imager
(1 to 200keV)
CdTe high density focal plane (CEA/IRFU) :
small pixel (300µm) 4 side buttable module
for large and high density focal planes
(reportés sur un support permettant de réduire la
densité en face arrière)
Hybridation haute densité
SDW Florence 2013 – A Bardoux

## Slide 12: Visible
SDW Florence 2013 – A Bardoux

## Slide 13: Visible detection : CCD
  No specific developpment in terms of scientific detectors
      CNES activity is focused on High speed TDI for High resolution pushbroom Earth observation (resolution below 70cm)
    Development of technogical blocks (at e2v) useful for future scientific detectors
      Large wafer backthinned
      Anti-etalon process
      Black coating
      Low noise on chip amplifier
      Close cooperation with ESA
SDW Florence 2013 – A Bardoux

## Slide 14: Visible Détection CMOS
  No specific developpment in terms of scientific detectors
      CNES activity is focused on High speed TDI for High resolution pushbroom Earth observation (below 70cm)
    same concern as ESA : setting up a whole supply chain whith good perennity
      Design house
      Foundry
      backthinning
      Assembly (space quality)
      Test and Space qualification
  Developpment of technological blocks that could be useful for scientific detectors
      CCD on CMOS , allowing TDI detection and CMOS readout
      Standard high performance »large » pixels (13 to 26µm pitch)
      Qualification of µlens and commercial component
    possible developpement for NEAT mission (Nearby Earth Astrometric Telescope)
SDW Florence 2013 – A Bardoux

## Slide 15: To know more about CMOS detectors
Workshop « CMOS for High
Free registration at :
https://cct.cnes.fr/content/workshop-cmos-image-sensors-high-performance-applications
Or contact me
alain.bardoux@cnes.fr
SDW Florence 2013 – A Bardoux

## Slide 16: Infra Red
SDW Florence 2013 – A Bardoux

## Slide 17: 2 main axis
Toward a large SWIR high performance detector (in coordination with ESA)
Toward a LWIR detector for Echo mission
Other activity
- Test of MCT APD
SDW Florence 2013 – A Bardoux

## Slide 18: Large SWIR detectors
  Several activities
  Improvement of manufacturing yield of large detectors
    detection wafer size increasing,
    hybridization reliability improvement
  Development of a low noise readout circuit
  Combined with a detection circuit impoved by ESA activity
  -> prototype
SDW Florence 2013 – A Bardoux

## Slide 19: high performance SWIR

## Slide 20: Echo mission
EChO (Exoplanet Characterisation Observatory; Cosmic Vision theme 1 - What are the conditions for planet formation and the emergence of life?) - a mission to investigate exoplanetary atmospheres, addressing the suitability of those planets for life and placing our Solar System in context
      Domain 5-12µm (French contribution)
      Driver : Dark current < 500é/s
      Technology : optimized HgCdTe
-
SDW Florence 2013 – A Bardoux

## Slide 21: Developments for EChO
4 detectors already fabricated and tested at CEA (LETI/Irfu) for temperature between 80 and 30K :
  1 detector fabricated with « standard » p/n technology
  3 detector fabricated with « optimisated » p/n technology
A large amount of pixels (on a detector) compliant with the need (< 500 e-/s) thanks to the optimised process.
Other wafer batch (p/n optimised process
at CEA Leti) under progress to provide 8 detectors to be tested by CEA Irfu
SDW Florence 2013 – A Bardoux

## Slide 22: Submm & mm
SDW Florence 2013 – A Bardoux

## Slide 23: Scientific missions in submm- mm
- Post Planck mission
  spectral domaine simililar to Plank one Planck (100, 143, 217, 353, 545 et 857 GHz ie, 350 µm to 3 mm)
  several technology candidate
  TES (NbSi) arrays
  LEKID arrays
  LETI all Solocon technology
Main drivers
Matrix development to improve performance and field of view
Collective manufacturing
SDW Florence 2013 – A Bardoux
Notes: Cosmologie : mm polarisatiob find diffus
Structurationd el’univers (suite Herschel)

## Slide 24: TES
pixel has 3 main functions
  Absorber (wavelength quarter cavity, antenna,…)
  Senseur is a supra bolometer (TES)
  Thermal insulation
MUX à SQUID senseur TES
SDW Florence 2013 – A Bardoux

## Slide 25: NbSi TES
NEP~5.10-17 W/Hz 1/2
SDW Florence 2013 – A Bardoux
Notes: TES faible impedance : SQUID ; APC a fait integraton et a dvpé un Asic
DCMB senseur NbSi quron depose, puis on structure pour faire membrane
Det 350 mK et etage deporté pour sauvegarder budget thermiqe

## Slide 26: LEKIDS (Lumped Element Kinetic Inductance Detectors )
LEKID (Lumped element Kinetic Inductance Detector) is based on inductance variation of a supraconductor film wrt incident power : resonnant frequency variation
one metal layer on a silicon substrate
No MUX required !
SDW Florence 2013 – A Bardoux
Notes: LE KID circuit resonnat associé a chaque pixele.
Ligne µonde
Chaque det a sa propre resonnace
Sous effet rayonnement shift de la freq de resonnance (et aussi amplitude)
Av : pas besoin de mux mourd

## Slide 27: LEKID realization
a 144-pixel Aluminum array was fabricated and tested in a dilution fridge with optical access, yielding an average optical NEP of ~2E-16 W/Hz^1/2 (best pixels showed NEP = 6E-17 W/Hz^1/2 under 4-8 pW loading per pixel).
A second prototype of LEKIDs has been tested at the IRAM 30 m telescope. A new LEKID geometry for 2 polarizations will be presented. Also first optical measurements of a titanium nitride array.
Well asapted for 1mm-3mm range
SDW Florence 2013 – A Bardoux

## Slide 28: Conclusion

## Slide 29
Annunciation by Leonardo da Vinci
Galleria degli Uffizi - Florence

## Slide 30
THANKS FOR YOUR ATTENTION