## Slide 1: Superlattice-doped Imaging Detectors Structure, Physics, and Performance
M. E. Hoenk, A. Carver, T. Jones, M. Dickie, and S. Nikzad
Jet Propulsion Laboratory
California Institute of Technology
J. Sgro
Alacron, Inc.
S. Tsur
Applied Materials Inc., Product Development Division, Israel
National Aeronautics and Space Administration
The work described here was carried out by the Jet Propulsion Laboratory, California Institute of Technology, under a contract with the National Aeronautics and Space Administration.
© 2013. All rights reserved.
Scientific Detectors Workshop
Florence Italy
October 11, 2013

## Slide 2: Outline
Instability of 3D doped detectors
Stability of 2D doped detectors
DUV lifetime test with pulsed laser irradiation
Practical Issues

## Slide 3: Instability of 3D-doped detectors

## Slide 4: Damage to EUV CCD on SOHO
J. M. Defise, J. D. Moses, Frédéric Clettec,and the EIT Consortium, “In-orbit performances of the EIT instrument on-board SOHO and intercalibration with the EIT Calroc Sounding rocket program,” Proc. SPIE 3442, Missions to the Sun II, 126 (November 2, 1998)

## Slide 5
Quantum Efficiency Hysteresis on Hubble
Light pipe added to WF/PC instrument to expose detectors to UV from sunlight
QEH mitigation: WF/PC 1 retrofitted for on-orbit UV flood
Janesick et al., “Scientific Charge Coupled Devices,” Optical Engeering, 26(8): 692-714, August1987.

## Slide 6: 3D Doping and The Dead Layer
-
Radiation damage causes instability and failure
Fermi level
+
+
Dead Layer
Interface traps (Dit)
Depletion region
Surface
Detector bulk
Mostly
Notes: Eliminating the traps is not enough – still have to stabilize the surface

## Slide 7: Quantum Efficiency Hysteresis and Backside Charging
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Positive charge  Depletion
Negative charge  Accumulation
+
+
+
+
+
+
+
+
+
+
+
+
+
3D doping forces a tradeoff between efficiency and stability
Depletion region
Surface
Detector bulk

## Slide 8: Stability and High QE of 2D doped detectors

## Slide 9
Delta doping for Surface Passivation
Self-ordered surface phase:
Boron on Silicon <100>
2D doping  Delta-doping
Dopant density as high as 1022cm-3
Hoenk et al., Applied Physics Letters, 61: 1084 (1992)
Fully-processed devices are modified using Molecular Beam Epitaxy (MBE)
MBE growth
3 nm
Delta-doped layer
(dopant in single atomic layer)
Native oxide
1 nm
original Si
CCD
frontside
circuitry

## Slide 10: Photometric Stability of Delta-doped CCDs
Standard Deviation (ppm)
J. M. Jenkins, W. J. Borucki, E. W. Dunham, J. S. McDonald “High Precision Photometry with Back-Illuminated CCDs,” ASP Conf Ser ,16-18 Oct. 1996 STScI
…the [delta-doped] CCD performed as a nearly shot-limited photometer with only a few ppm of error at a flux level of 1010e- per sample

## Slide 11: Damage Ultraviolet Damage
Very high interface trap densities are possible
  Passivated thermal oxide: n2D ~ 1010 cm-2eV-1
  Thermal oxide “as-grown”: n2D ~ 1012 cm-2eV-1
  Damaged oxide: n2D ~ 1014 cm-2eV-1
References:
  Afanas’ev, V.V., de Nijs, J. M. M., and Balk, P., “Degradation of the thermal oxide of the Si/SiO2/Al system due to vacuum ultraviolet radiation,” J. Appl. Phys., 78(11): 6481-6490, 1995.
  Arp, U., Shaw, P.S., Gupta, R. and Lykke, K.R., “Damage to solid-state photodiodes by vacuum ultraviolet radiation,” J. Electron Spectroscopy and Related Phenomena, 144-147: 1039-1042, 2005.
  Li, FM & Nathan, A, “CCD image sensors in deep-ultraviolet: degradation behavior and damage mechanisms,” Springer, Berlin, 2005.

## Slide 12: Surface Passivation by Quantum Exclusion
“Surface Passivation by Quantum Exclusion Using Multiple Layers,”
Michael E. Hoenk, U.S. Patent 8,395,243, issued March 12, 2013.
Structure
  2D-doping Superlattice
  Self-organized boron surface phases
  Equivalent density > 1021cm-3
Physics
  Quantum confinement
  Quantum transport
Performance
  Near 100% internal QE
  Stable against several billion pulses of high intensity DUV laser radiation
Notes: Delta-doping = Single 2D doped layer
Superlattice = Multilayer 2D doping

## Slide 13: Surface Passivation by Quantum Exclusion
Conduction band
Valence band
Electron subband
Hole subbands
Bulk
Surface
Bulk
Surface
Super- lattice
Bulk
Surface
SL
  Quantum confinement eliminates dead layer
  Ballistic transport suppresses recombination of hot carriers
-
+

## Slide 14: Dead layer vs. Trap density
3D doping
2D doping

## Slide 15: DUV Lifetime Tests Superlattice vs. Laser

## Slide 16
Aerial Imaging Mask Inspection System
Mask defect
(SEM)
Wafer defect
(SEM)
Wafer defect
(Aerial)
Applied Aera2™
Mask inspection imaging optics.

## Slide 17
Lifetime Testing with Pulsed DUV Lasers

## Slide 18: Calibrating DUV laser damage with test wafers
Traps decrease conductivity
Trap density ~ 1014 cm-2eV-1

## Slide 19
Pulsed 263 nm laser up to x257 camera saturations
QE = 64% with AR-coated sensor – 28nm Al2O3
QE and dark current stable to maximum tested dose (3.1 kJ/cm2)
No blooming and no image memory were present even at the high saturation levels.
High modulation transfer function (MTF)
263nm Results
Superlattice-doped detector stability

## Slide 20
Normalized Spatial Response following 2.1 B pulses
Exposure slit position on sensor
193nm Results
>2 Billion laser pulses at full saturation
No measureable change (within +1%)
Estimated Lifetime > 10B laser pulses.
Internal QE ~100% (excluding Quantum Yield)
No blooming and no image memory at 1000 fps.
Superlattice-doped detector stability

## Slide 21: Practical issues

## Slide 22
Charge-coupled Device (CCD)
Serial readout device with charge transfer and one (or few) readout amplifiers.
CMOS APS Imaging Array
Parallel readout with few charge transfers and one readout amplifier per pixel.
Versatility of 2D Passivation
CCD
CMOS APS
Superlattice doping has been demonstrated on CCDs (multiple types), CMOS APS imaging arrays, photodiode arrays, and fully-depleted photodiodes.
Notes: 22
Delta-doping is equally applicable to back-illuminated CCDs and CMOS imaging arrays.

## Slide 23: Wafer-scale Superlattice Doping
Veeco 8-inch Silicon MBE at JPL’s Microdevices Lab
8-inch CMOS wafer during MBE growth at JPL’s Microdevices Lab
High throughput production of superlattice-doped, 200 mm wafers

## Slide 24
Technology Transfer
“Surface Passivation by Quantum Exclusion Using Multiple Layers,”
Michael E. Hoenk, U.S. Patent 8,395,243, issued March 12, 2013.
Alacron Inc. BSI DUV camera with superlattice-doped, AR-coated CMOS imaging array.

## Slide 25: Conclusions
  Instabilities of 3D doping
    Quantum efficiency hysteresis and the “mostly dead” layer
    Radiation-induced interface traps
  Stability of 2D doping
    Near 100% internal QE, no QE hysteresis
    Quantum exclusion eliminates trapping and surface recombination
  DUV lifetime tests superlattice-doped CMOS
    Insensitive to surface traps and DUV damage ~ 1014cm-2eV-1
    193nm: STABLE at >2 Billion laser pulses at full saturation
    263nm: STABLE at >2 Billion laser pulses at 257x saturation
  Practical matters
    Versatile
    Manufacturable
    Technology transfer
We are very interested in partnerships for development, delivery, and deployment of high performance detectors.