## Slide 1
CCD and CMOS X-ray Detector Development for Synchrotron and Space Applications
Andrew Holland1,2, D. Hall1, M. Soman1, K. Stefanov1, K. Holland2, P. Jerram3
Centre For Electronic Imaging, Open University, UK (www.open.ac.uk/cei)
XCAM Ltd., Northampton, UK (www.xcam.co.uk)
Teledyne e2v, Chelmsford, UK (www.e2v.com)

## Slide 2: X-ray Photon Events in Pixel Detectors
Absorption in depletion region leads to be isolated single/double events
Absorption in field-free region leads to multi-pixel spread events

## Slide 3: High Resolution Spectroscopy using a CCD
Composite spectrum from e2v CCD12
nelectrons = E/w (300eV@80 e-)
variance = FE/w (V100e-=12e-)
(Fano factor, F=0.12)
Requires photon-counting mode
“Fano-limited” resolution

## Slide 4: Imaging vs. Dispersive Spectrometer
XMM EPIC/MOS
XMM RGS
Imaging
Spectroscopy
High Resolution Spectroscopy

## Slide 5: CMOS Image Sensors for X-ray Detection
e2v CIS115 is being developed for JUICE for visible imaging of Jupiter’s moons
  Back-illuminated, 9-12mm thick
  3 Mpixel, read through 4 blocks
  7 mm pixel pitch
  Area = 1.4 cm2
  R=48mV/e-
  Noise 4-5 e- rms.
  Qualified to 250 krad TID

## Slide 6: X-ray spectroscopy with CIS115
Recent results using Fe-55 from the calibration data of Matt Soman
Will enable 7mm and below spatial resolution
Around 60% of events could undergo centroiding to increase resolution further
Probably all sub-keV X-rays may be split
QE is currently low (device thickness) and no samples without AR coating
Accuracy 7mm
<7mm

## Slide 7: CIS115 Split event fractions
With this sensor variant, the majority of photon events are split (note @6keV)
This enables event centroiding and hence higher resolution than the pixel size
However, this also degrades non-dispersed photon counting spectroscopy (which would require thick/full depletion)

## Slide 8: Fully Depleted CCDs
Thick fully-depleted CCDs have been available for a few years
CCD261 – 2kx4k format
200 mm thick with full depletion
BB=0V
BB=-15V

## Slide 9: CMOS QE Improvement using Full Depletion
JUICE CIS115 sensors have ~5 mm depletion on 10 mm BI structure
Restricted efficiency for X-ray use
Can obtain up to ~40mm BI devices on epi-Si
Test structures have been developed at OU and fabricated by ESPROS
Device are currently being evaluated under a PhD studentship
This development may go part-way toward making a useful X-ray detector using a standard CMOS process
CMOS
CCD

## Slide 10: Development of a Pinned Photodiode CMOS Image sensor with Reverse Substrate Bias
Would like a fully-depleted + thick CMOS sensor
Problem of current flow when applying back-bias (i.e. making an expensive resistor!)
Working on DDE technology
Backed up by comprehensive 2&3D modelling

## Slide 11: The DDE (deep depletion extension)
Test structures have been fabricated
The DDE principle has been demonstrated
The result may look fairly innocent… but!
This opens up the route toward fully-depleted CMOS image sensors
  CMOS foundry process
  100-200 mm active thickness

## Slide 12: CMOS QE Improvement - toward Full Depletion
To make significant improvements need to use bulk FZ silicon
& use reverse bias for full depletion
Supported by patent
First prototypes show very promising performance
Complementing established CMOS properties
  Pinned photodiode for low noise
  High speed and low power readout
  Radiation hardness
Will improve both X-ray and IR QE for future CMOS devices

## Slide 13: The EM CCDs for Soft X-ray Detection
Rf1
Rf2
Rf3
If1
If2
If3
multiplication
register
Rf2HV
A standard CCD becomes an EMCCD by the insertion of a

## Slide 14: EM CCD Gain
The multiplication register utilises impact ionisation in 536 multiplication elements with each electron having a small chance of increasing the charge in each element.
A common issue with faster readouts is larger readout noise. EM-CCDs supress this larger noise due to the multiplication register increasing the signal sufficiently high enough allowing for faster reads.
Gain=(Gain/stage)Nelements
Eg (1.01)536 = 207x.
If the noise is s=50 e- rms. e.n.c.=50/207 = 0.24 e- rms.

## Slide 15: EM-CCDs giving increases SNR
Gain = 1
Gain = 7
1.0 keV
0.3 keV
Improved detectability

## Slide 16: X-rays in an EM CCD
EM gain can enable the CCDs to be read out with at high speed, with high noise, yet with low e.n.c.
Modified Fano factor - v = (1+F)E/w due to shot noise on avalanche process
Sub-pixel charge centroiding can increase spatial resolution
Example of an Mn-K X-ray
  Signal occupies ~12-16 pixels
  S/N~1000:1
  Enables centroiding to ~1 mm

## Slide 17: Soft X-ray QE Measurements
Since XMM, the CCD production and BI processing at e2v has been changed..
This programme was aimed at re-characterising the soft X-ray performance of the current build standards of the e2v BI process
Both Standard and Enhanced BI processes were evaluated
Custom CCD97s were produced
50-2000 eV range

## Slide 18: Soft X-ray QE Measurements at PTB
Measurements were taken on 2 devices of each type
Results were used to develop new modelling
Results are described in an e2v “White Paper” https://www.e2v.com/products/imaging/technical-papers/
Basic Process
Enhanced Process

## Slide 19: Light Blocking Filter Development
We have been developing new direct-deposited light blocking filters on BI CCDs
Explored a range of build configurations on a CCD97 test vehicle
Light filter put in place of the conventional store shield
Quantified the optical transmission including pinholes
Tested at the PTB facility at Bessy II for X-ray transmission

## Slide 20: Light Blocking Filter Measurements
Optical transmission and X-ray transmission results
Further qualification of the process is being considered for the SMILE project

## Slide 21: Current Applications Being Developed
X-ray Dispersive Spectroscopy
  RIXS Camera System
  OGRE Sounding rocket experiment
X-ray Imaging
  SMILE SXI

## Slide 22
RIXSCam During Assembly & Test
For improved readout of dispersed X-ray grating spectrometers
XCAM has developed a camera system for RIXS using EM CCD207-40s & event centroiding
Triple-CCD camera system during assembly
Is fabricated as 3 independent camera systems, but with a master clock for synchronisation

## Slide 23
Soft X-rays in the RIXSCam
For soft X-rays in BI device photons are absorbed close to the entrance window
Majority of X-ray events undergo lateral diffusion during drift to potential wells
Recent results using the RISCCam from PSI/SAXES for a de-focussed line
460 eV photons with high S:N
Centroiding to 2 mm FWHM

## Slide 24
RIXSCam Early Commissioning Results
Example of an accumulated spectrum
The RIXSCamTM includes the RIXS dll which performs the on-the-fly event centroiding and eta-correction to give the high spatial resolution
Correction for diffraction curvature
Integrates into EPICs
Stack of 100 images
Centroided photons

## Slide 25
OGRE Sounding Rocket Experiment
Testing a high resolution (R~3000) grating spectrometer
Launch (currently) scheduled for Feb. 2020
XCAM-OU responsible for developing the X-ray camera to read out the spectrum
Aimed at raising the TRL of the system components

## Slide 26
Prototype OGRE Camera System
Prototype camera electronics Laboratory CCD array
Testing a high resolution (R~3000) grating spectrometer
Launch (currently) scheduled for Feb. 2020
XCAM-OU responsible for developing the X-ray camera to read out the spectrum.
Aimed at raising the TRL of the system components

## Slide 27
OGRE Performance Simulations
Current configuration of the OGRE optics system is shown on the right
During launch the payload will image Capella for ~5 minutes
Models of the measured X-ray spectrum are given below
Grating
Detector
Mirror

## Slide 28
PX-ray = α nsw usw nn
X-ray power depends on SW density
and velocity and exosphere density
Aq+ + B → A(q-1)+* + B+
A(q-1)+* → A(q-1)+ + hν
Solar Wind Charge Exchange:
Heavy solar wind ions in collision
with neutral geocoronal atoms
The Earth through X-ray spectacles
nn ~ R-3

## Slide 29
Q3 2021

## Slide 30: Soft X-ray Imager on SMILE
T. Sun (NSSC)
Lobster-eye Micropore Optic
Ultra-wide field of view
~16° x 27°
Focal length 30 cm
Optic Mass < 1kg
Instrument ~ 26 kg
SXI FOV
UVI
FOV
PLM
SVM
PM

## Slide 31: SXI CCD Configuration
Based on the PLATO CCD270 mask set
Optimised as an X-ray detector and not an optical imager
Image 3791 rows
  6x binned at store IF
  631 rows
  5 CI rows
Store 719 rows
  87 spare rows

## Slide 32: Radiation Damage in CCD270s
Once again, radiation damage is becoming a concern in the CCD270 for SMILE
A combination of limited radiation shielding and large CCD area compounds the problem
Radiation damage modelling and characterisation will need to be improved to meet the mission requirements
bottom
~row 1500
top
~row 3000

## Slide 33: Silvaco Modelling
Suggested SBC with 4 um width in the parallel direction for improved radiation hardness

## Slide 34: Dynamic Modelling of the SBC
We have recently created dynamic simulations of charge flow in the proposed SBC for the SXI CCDs
Concerns that the charge may “balloon” beyond the SBC confinement into the normal channel seem un-founded
Indicates that the improved radiation hardness will be maintained during transfer

## Slide 35: SXI Performance Modelling over Time
Radiation damage in these large CCDs is one of the key challenges
We are modelling anticipated performance over time
Further improvement arising from charge injection and lower operating temperature
Also responsible for development of in-flight correction software
The aim is to delay the operational period at which we start to lose photons…

## Slide 36: Talk Summary
We continue to develop silicon CCD and CMOS image sensors for direct X-ray detection
We are currently developing a new generation of CMOS sensors capable of being fully-depleted to 100-200 mm
Optical light blocking filters are being developed
QE and transmission data is refining QE models
These developments are finding their way into new science applications (and hopefully more to come…)