## Slide 1
September , 2017
Presented by Richard Demers
Coronagraph Flight Systems Manager
Jet Propulsion Laboratory
The EMCCD as imaging and spectrograph sensor for the WFIRST Coronagraph Instrument
© 2017 California Institute of Technology, All rights reserved, Government sponsorship acknowledged

## Slide 2
Patrick Morrissey, Leon Harding, Michael Bottom, Bobby Effinger, Leo Neat, Richard Demers
Jet Propulsion Laboratory
Nathan Bush, David Hall, Andrew Clarke, Ross Burgon, Andrew Holland
Open University, Center for Electronic Imaging
Bijan Nemati
University of Alabama at Huntsville
WFIRST Coronagraph Camera Team & Co-authors

## Slide 3: Outline
WFIRST
What is a coronagraph?
WFIRST Coronagraph cameras
  Science cameras
  LOWFS camera
Radiation testing
Planned design mods
Conclusion

## Slide 4: WFIRST Summary
WFIRST = Wide Field InfraRed Survey Telescope
    2.5 Meter Telescope
    Wide Field Instrument
    Coronagraph Instrument
Coronagraph Science
  Atmospheric compositions of planets
  Characterize debris disks around nearby stars
  Direct Exo-planet imaging
Pre-Decisional Information -- For Planning and Discussion Purposes Only
Notes: CGI does not drive mission cost/schedule
WFI – cosmic acceleration and structure

## Slide 5: Coronagraph Unique Status
Both a science instrument & technology demonstration
Baseline Science Requirements
  Designed & costed to meet science requirements
Threshold Technology Requirements
  Advances critical technology for future missions
WFIRST CGI is the only activity planned by NASA to image and spectrally characterize exoplanets for the next decade
Xinetics 48 x 48 DM used in JPL’s HCIT
E2V EMCCD used in photon-counting mode
HLC mask image with an atomic force microscope
Fast-steering mirror

## Slide 6: WFIRST Coronagraph Team
Coronagraph partner institutions:
NASA GSFC (provided test-bed integral field spectrograph)
Science Centers:
    IPAC/Caltech, STScI

## Slide 7: CGI in WFIRST Payload
Payload, integrated
Imaging Optics
Assembly (IOA)
Wide-Field
Instrument (WFI)
Coronagraph
Instrument (CGI)
Instrument Carrier (IC)
Payload, exploded view
Tertiary Optical Mirror Assembly (TOMA)
Pre-Decisional Information -- For Planning and Discussion Purposes Only

## Slide 8
Diffraction
Focal plane
Diameter (D)
Wavelength (l)
Entrance Pupil
Log stretch
Unfortunately, the planet would be right here (and about 10 billion times dimmer)
Log stretch
Notes: Send these three slides to Feng.

## Slide 9
The Lyot Coronagraph
Entrance
pupil
Occulter
Lyot stop
Image
plane
Planet
light
Star
light
What happens when there is a planet?
The planet light goes through
the coronagraph unattenuated
by the occulter.

## Slide 10: A Coronagraph needs active optics
Deformable Mirrors
#1 and #2
Low Order Wavefront
Sensor
Masks, Apodizers, Stops
Flip Mirror
Integral Field
Spectrometer
IFS Detector
Post-processing
Imaging Detector
High–order wavefront control loop
LOS Pointing jitter rejection
(pointing stability)
Wavefront error drift rejection
(WF aberrations due to thermal changes and telescope attitude)
Light from star and planet
Telescope
Optics
Control
Detector
Post-processing
LOWFS Detector
IFS Detector
Disturbances
Wavefront & LOS
Jitter
Drift
Image Speckle
(WF aberrations due to imperfections in optics)
Tip/Tilt Mirror
Notes: Add loop for FocM

## Slide 11: Optical Module Bench
OAP3
Focus correction mirror
DM1
OAP2
DM2
Fold mirror
OAP1
Fast Steering Mirror
Aperture Cover
OAP6
Light incident on FSM from TOMA
Focal Plane Mask
Field Stop
OAP8
Color
Filter Wheel
IMG/Pupil/IFS Selection
Imaging Camera
IFS Optics
IFS Camera
Lyot Stop
OAP7
LOWFS Camera
OAP4
OAP5
Shaped-pupil mask
CCD201-20: 1K⤬2K format 13.3 ⤬ 26.6 mm
Light
Completely enclosed, 1cm Ta Shield Concept

## Slide 12: CGI Cameras
EMCCD enables high QE CCD imaging and zero read noise photon counting.
Low light level multi-stage serial register at elevated voltage (~50V) amplifies signals well above the level of the read noise.
Amplified data are sent to a photon counting discriminator, eliminating read noise.
Two science cameras
  Direct imaging camera (DICAM)
  Integral field spectrograph camera (IFSCAM)
One engineering camera
  LOWFS camera (LOCAM)
Science cameras detect ultra-low flux (~1 ph/pix/15 min)
  ~100 sec frames
LOWFS camera detects higher flux
  1kHz frame rate
Teledyne-e2V CCD201-20 baselined for CGI cameras
CCD201-20 version has been extensively tested
  Electro-optical parameters
  Radiation exposure
  Low flux image characterization
Notes: Articulate the low flux regime (~1 ph/10 min); low flux measurements
----Note from Documentarian (Mary)----
Formatting to continue 8/15 from Slide 21

## Slide 13: Camera Requirements
LOWFScam
  <5 e- read noise requirement
  50,000 e- full well requirement
  1000 fps operation of a 50x50 pixel region requirement
  Latency of <1ms requirement
DIcam/IFScam
  Minimum flux detection limit ~ 1 photon/pixel/15 min
  dQE ≳50% (TBR)at midlife, 95% confidence level
  Read noise (gain = 1, 1000) = 55, 75 e- RMS
  Dark current (BOL, EOL) < 1 , 2 e-/pix/hr
  CIC < 0.01 e-/pix/frame
COTS CCD201-20 meets requirements

## Slide 14: Radiation Test Program
WFIRST expected radiation environment at L2 (Kepler, JWST).
  This location is beyond the Moon and outside the protection of the Earth’s magnetosphere
  Radiation dose will be dominated by protons from solar flares.
EMCCD detectors exhibit charge transfer degradation (trap defects) similar to other CCD detectors (e.g. HST) when the lattice is damaged by energetic particles.
Collaboration with Open University, UK to evaluate the performance of commercial EMCCDs that are degraded by a flight-like radiation dose (95% confidence, 5 years, RDF=2) of protons.
Radiation Exposed areas
We have evaluated two sets of irradiated devices and determined that the damage is dominated by the image area.
EMCCD
Image
Store
Serial

## Slide 15: L2 Orbit Radiation Environment
Flare Distribution
Tested at this level
95% confidence
7 years
3 years
5
Modeled at this level

## Slide 16: Radiation Damage
Proton damage results in 1) hot pixels and 2) charge transfer degradation.
  Hot pixels may have much higher dark than the typical pixel (>10x), however, these pixels are ~10% of the total even at end of mission.
    The diffuse dark current remains under 1 electron-px-1-hour-1
  Charge transfer degradation due to traps disproportionately affects faint signals since traps are efficient when they are empty.
    Increasing the frame time is an effective mitigation but is limited by the long tails of cosmic rays generated in the EM gain register
Shielded
Damaged
Hot Pixels
Cosmic Rays
di-Vacancy traps, 50⤬50 window

## Slide 17: Radiation Induced Image Degradation
Low flux PSF measured using a scene generator and ND filters
PSF detection is characterized using
  Aperture photometry
  Markov Chain Monte Carlo Model
Input flux dependence of dQE is measured
The radiation-damaged detector performance at 5 years meets requirements. Desirable to increase performance margin by improving the sensor design at Teledyne-e2v.

## Slide 18: Trap mitigation: narrow channels
Narrowing the buried channel result:
Higher density charge packets for a given signal size
Smaller volume for a given signal size
Change in the position of signal(y-axis) related to the change in channel parameter
2x reduction in capture probability for 4u𝝁m channel width
Analysis by Nathan Bush of Open University, CEI

## Slide 19: Modeling of EMCCD Detector Improvements
What performance improvement is expected by narrowing the channel width of frame register pixels from 9um to 4um.
Result: The detector trap model predicts that signal loss due to radiation induced traps is decreased by a factor of 2 at a flux of 0.01 c-PSF-1-s-1 by narrowing the image pixel channel width from 9um to 4um.
Reducing the channel width further does not show much added benefit.
Fractional loss, (# e- lost / # in pre-read PSF)
~2x less signal loss with 4um channel width than 9um
Analysis results by Bobby Effinger, 8/16/2017
The effect of a 2x improvement of the detector CTI through narrowing the channel widths of the frame pixels is evaluated for the current error budget.
The margin against the detector requirements improves from 21% to 31%
Error Budget Items | Nominal Req. (ppb) | Nominal CBE (ppb) | 2x Impr. In CTI CBE (ppb)
Photometry Noise | 0.50 | 0.41 | 0.36
Detector Noise | 0.41 | 0.32 | 0.28
Margin against Detector Req. |  | 21.0% | 30.9%
EB results by Bijan Nemati, 8/16/2017

## Slide 20: Planned Device modifications
Step 1 : Low risk fast turn around approach (process change only)
Eliminate visible light shield in store section
Reduces number of transfers to serial readout by ~1000 transfers
Image camera only needs small window
Step 2 : More aggressive approach (both process and design change)
Two different buried channel reduced widths (3, 4 𝜇m) in a banded array
Notch channel design (high heritage)
Overspill register drain dump
High responsivity/low noise output amp
Store Section
1056H×1037V elements

## Slide 21: Summary
EMCCD technology is being advanced for the WFIRST CGI
  Low flux image and characterization
  High frame rate wavefront sensing
Ambient and cryo-radiation testing was completed
  Characterized dark current, CIC, image degradation in the presence of displacement damage
COTS EMCCD meets performance requirements
  Various modifications are underway to increase margins
Next programmatic milestones
  System Requirements Review
  Subsystem Definition Review
GPI image of 51 Erdiani b, Courtesy Bruce Macintosh, Stanford University

## Slide 22: High Contrast Spectrum - GPI
GPI image (2015) of 51 Erdiani b, provided by Bruce Macintosh, Rob deRosa & Christian Marois, UC Berkeley

## Slide 23
RESERVE SLIDES

## Slide 24
The Apodized Pupil Coronagraph
Slide courtesy of A. Give’on

## Slide 25: Cryo Radiation Test Summary
Parameter | Units | Org. | Pre-Irradiation | Post-Irradiation 2.5✕109 pr/cm2 | MS-7 Requirement
Image area Dark Current | e-/pix/sec | JPL | (3.00±0.40)×10-5 | (7.00±0.0)×10-4 | 1.0×10-3
Effective Read Noise | e-/pix/frame | JPL | (1.70±0.0)×10-6 | (1.70±0.0)×10-6 | 1.0
Total CIC | e-/pix/frame | JPL | (2.1±0.2)×10-3 | (2.3±0.2)×10-3 | __
EPER Parallel CTI (10e- signal) | - | CEI | (8.88±0.49)×10-6 | (8.32±0.52)×10-4 | __
EPER Serial CTI (10e- signal) | - | CEI | (1.65±0.47)×10-5 | (6.84±0.15)×10-4 | __
X-Ray Parallel CTI (1 event/2700 pix) | - | CEI | (0.569±1.0)×10-6 | (1.31±0.05)×10-4 | __
X-Ray Serial CTI (1 event/2700 pix) | - | CEI | (1.65±2.08)×10-6 | (4.12±0.35)×10-5 | __
NOTES
1. CEI measurements made at 165K using XCAM commercial electronics, not performance optimized
2. JPL measurements made at 168K using NüVü flight-like commercial electronics, performance optimized
3. CEI read noise measurement (not shown) made in analog mode with low gain
4. JPL read noise measurement made in photon counting mode with high gain
5. JPL EOL measurements are optimized for extremely low flux detection and result in slightly higher dark current.
25

## Slide 26: CGI Modes – Hybrid Lyot
Pupil mask
Lyot
mask
Filter
wheel
Field stop
mask
to LOWFS
FSM
OAP5
OAP6
OAP7
OAP8
DM2
FocM
OAP1
OAP2
OAP3
DM1
FM
IFS/Img Selector
Focal Plane mask
FPA
IMG
Hybrid Lyot Mode
360deg dark hole from 3 to10 lambda/D for planet photometry and discovery
Coronagraph Instrument (CGI)
OAP4
M4
F1
F1
F2
Tertiary Collimator Assembly (TCA)
Telescope
PM
SM
F3
F2
POMA
TOMA
M3
Notes: Say something about autonomous operation firsts.
Ask J Krist to remove contrast values.

## Slide 27: CGI Modes – Shaped Pupil Spectroscopy
Pupil mask
Lyot
mask
Filter
wheel
Field stop
mask
DM2
FocM
DM1
FM
IFS/Img Selector
Focal Plane mask
Shaped Pupil Spectroscopy Mode
FPA
IFS
IFS
to LOWFS
The IFS uses 3 18% bands to produce R=50 spectra from 600 to 970nm
lenslet array
pinhole mask
dispersed lenslet images
extracted data cube
SPC images in 3 18% bands
Coronagraph Instrument (CGI)
OAP5
OAP6
OAP7
OAP8
OAP1
OAP2
OAP3
OAP4
FSM
M4
F1
F1
F2
Tertiary Collimator Assembly (TCA)
Telescope
PM
SM
F3
F2
POMA
TOMA
M3
Notes: Actuated TCA mirror?

## Slide 28: CGI Modes – Shaped Pupil Disk
Pupil mask
Lyot
mask
Filter
wheel
Field stop
mask
DM2
FocM
DM1
FM
IFS/Img Selector
Focal Plane mask
Shaped Pupil Disk Imaging Mode
to LOWFS
Disk Imaging at wavelengths 508 and 721 nm, with OWA of 20 lambda/D
Coronagraph Instrument (CGI)
FPA
IMG
Image from 2015 Exo-C STDT Final Report
OAP5
OAP6
OAP7
OAP8
OAP1
OAP2
OAP3
OAP4
M4
F1
F1
F2
Tertiary Collimator Assembly (TCA)
Telescope
PM
SM
F3
F2
FSM
POMA
TOMA
M3

## Slide 29: T-e2V CCD201-20 Architecture
Frame transfer configuration
High Responsivity (HR) output – conventional CCD operation
Large Signal (LS) output – EM gain operation
Standard & Corner elements
  Bend-around to reduce die size
  468 selected to balance the 1056 element row and thus act as buffer (with 604 elements) to increase readout speed
Taken from Harding & Demers, et al. (2016)
29

## Slide 30: 1st Actively Controlled Optical Imaging Instrument w/ Coronagraph Masks in Space
Active components
  Fast steering mirror (FSM) for line-of-sight control
  Focus correction mechanism (FocM) for focus control
  Deformable mirrors (DM1, DM2) for wavefront error control
Control loops
  High-order wavefront sensing control (HOWFS/C) loop for initially achieving starlight suppression
  Low-order wavefront sensing control (LOWFS/C) loop for continuously maintaining starlight suppression

## Slide 31: Acronyms
CGI = Coronagraph Instrument
DICAM = Direct Imaging Camera
DM = Deformable Mirror
FocM = Focus Control Mechanism
FSM = Fast Steering Mirror
FSW = Flight Software
I/C = Interface Card
IFS = Integral Field Spectrograph
IFSCAM = IFS CAMera
LOCAM = Low Order wavefront sensor CAMera
OAP = Off-Axis Parabola
OTA = Optical Telescope Assembly
PCU = Power Conditioning Unit
POMA = PickOff Mirror Assembly
TOMA = Tertiary Optical Mirror Assembly
TCA = Tertiary Collimator Assembly
MECHANISMS
SPWM = Shaped Pupil Wheel Mechanism
OCWM = Occulter Wheel Mechanism
LSWM = Lyot Stop Wheel Mechanism
FSWM = Field Stop Wheel Mechanism
CFWM = Color Filter Wheel Mechanism
CSWM = Camera Selector Wheel Mechanism

## Slide 32: Radiation Testing : Phase I Single Displacement Damage Dose (DDD)
Single exposure of Displacement Damage Dose (DDD) at room temperature
Survivability test of detector for 2.5 x 109 protons cm-2 dose [10 MeV equivalent]
  ~Corresponds to 6 years at L2 orbit with Ta shielding
DUT engineering-grade EMCCD: e2V m/n CCD201-20
Paul Scherrer Institute Beamline, Switzerland in April 2015
Assessed degradation of:
  Read Noise, EM gain, Clock Induced Charge, Dark current, Charge Transfer Inefficiency
T = 293 K during irradiation;
165 ±2 K during post exposure measurement
Unbiased during exposure
Frame time = 100 sec
Inverted Mode Operation (IMO): suppression of large surface dark current
Serial readout rate of 700kHz (some exceptions)
Exposed areas
DUT = device under test
32

## Slide 33: Radiation Testing: Phase II Incremental Displacement Damage Dose (DDD) at Cryo
Four separate exposures of Displacement Damage Dose (DDD) at cryo-temp
  Characterize the performance degradation at intermediate points in 6 year life cycle
DUT science-grade EMCCD: e2V m/n CCD201-20
  Performance fully characterized before campaign and after each of four doses
Facility: Helios 3 Beamline, Harwell, UK
T = 165 ±2 K for irradiation; (±5 K during measurements)
Biased during exposure to monitor flatband voltage shift
Inverted Mode Operation (IMO): suppression of large surface dark current
Serial readout rate of 700kHz (some exceptions)
Applied bias voltages during test same as for Phase I for comparison*
  * Except for the two voltages driving EM gain
Exposure Dose [109 protons/cm-2] | Cumulative Dose [109 protons/cm-2]
0 | 0
1 | 1
1.5 | 2.5
2.5 | 5
2.5 | 7.5
Four cumulative doses summing to 7.5 x 109 pr/cm2 [10 MeV equivalent]
  Fourth dose smaller than prescribed due to facility failure
    Reported but not used in analysis
  Performance fully characterized before campaign and after each of four doses
    Dark current, CIC, EM gain, RN, X-ray CTI, EPER, amplifier responsivity
33

## Slide 34: Rad-hard modifications