## Slide 1: Flat Field Forensics
Timothee Greffe
28 of September. 2017

## Slide 2: e2v 231 CCD 6k*6k
4 x 4 array on Zwicky Transient Facility
  4 outputs:
    only the two upper ones are used on the following work.
  4 phase parallel clocking.
  800kHz pixel clock
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion

## Slide 3: Outline
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Parallel Transfer
  Photon Transfer Curve Dip and pixel shifting
  Transfer inefficiency
Surface Well
  Analysis and improvement
Pixel Response Non Uniformity
  From 2 phases to 3 phases
  Lithographic mask
Conclusion
NGC7331 @ Palomar Observatory – P200 using the e2v ccd-231

## Slide 4: Parallel Transfer
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Parallel Transfer

## Slide 5: Photon Transfer Curve
Flattening of the PTC for high levels
  Surface Well effect?
  Lateral diffusion (Brighter-Fatter effect)?
          … maybe both?
0V
15V
Voltage
distance
  Surface Well occurs when charges are hitting the Si-SiO2 surface
-5V
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
0V
10V
Voltage
distance
-5V
Surface Well

## Slide 6: Photon Transfer Curve - Tuning
A broad range of voltages is explored to find the best setting.
  => more than 90 PTCs!
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Dip
A class of PTC with unexplained dip appears

## Slide 7: “Downing Dip”
A look-alike dip was first described in a paper from Mark Downing.
We decided to focus on this strange behavior:
  It may lead to interesting discovery.
  It improves our understanding of the CCD.
Extract from “Bulk Silicon CCDs, Point Spread Function and Photon Transfer Curves: CCD testing activities at ESO”
Mark Downing et al.
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Extract from “Electro-Optical Testing of Fully Depleted CCD Image sensors for the Large Synoptic Survey Telescope Camera”
Peter E. Doherty et al.
Dip
Dip
Dip

## Slide 8: Hypothesis: Image shifting
What if the whole image area drifts when the level increases?
C,σC
If some correlated noise
1
1
0.5
Additive term null in 0 and 1
0.5
What is the resulting noise of a frame C made of two equivalent frames A and B partially summed?
No drift
Fully drifted
Half drifted
0
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
1 pixel
Voltage Swing on parallel clocks: -4V to 2V

## Slide 9: Cross-Correlation
Cross correlation frame to frame is computed to spot the drift
  It relies on the FPN on the Image Area.
Reference level for Cross-Correlation
There is indeed a drift of the whole image area during the “Downing Dip”
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion

## Slide 10: Cross-Correlation
Cross correlation frame to frame is computed to spot the drift
  It relies on the FPN on the Image Area.
Reference level for Cross-Correlation
There is indeed a drift of the whole image area during the “Downing Dip”
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
But HOW is this happening?

## Slide 11: Mechanism: How it should work.
TGD | IPHI4 | IPHI3 | IPHI2 | IPHI1 | IPHI4 | IPHI3 | IPHI2 | IPHI1
Time
Serial Register
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Pixel 1
Pixel 2
Transfer Gate and IPHI1 tied together

## Slide 12: Mechanism: What if the last node is missing?
TGD | IPHI4 | IPHI3 | IPHI2 | IPHI1 | IPHI4 | IPHI3 | IPHI2 | IPHI1
Time
Serial Register
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Pixel 1
Pixel 2

## Slide 13: Mechanism: When the charges are spilling into the serial register?
TGD | IPHI3 | IPHI2 | IPHI1 | IPHI4 | IPHI3 | IPHI2 | IPHI1
Time
Serial Register
?
?
?
?
?
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Pixel 1
Pixel 2

## Slide 14: Mechanism: 2 cases
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Pixel 1
Pixel 2
Pixel 1
Pixel 2
Lower light levels: Pixel 1 is read
Higher light levels: Pixel 2 is read => Translation

## Slide 15: Electric field shaping
Reason why charges are flowing or not for a given level into the serial register is still unexplained.
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Hypothesis: Charges shape the electric field.
    potential wall could appear or disappear at the edge between image area and serial register.
    Phenomenon with a threshold effect.
Serial Register
Potential
Transfer Gate
I Phi 3
I Phi 2
I Phi 1
I Phi 4
Wall
Serial Register
Potential
Transfer Gate
No more Wall: every charges flow to the serial register
charges
I Phi 3
I Phi 2
I Phi 1
I Phi 4

## Slide 16: Mechanism: New clocking scheme
TGD | IPHI3 | IPHI2 | IPHI1 | IPHI4 | IPHI3 | IPHI2 | IPHI1
Time
Serial Register
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Pixel 1
Pixel 2
Transfer Gate rises and falls earlier than previously.
=> Concurrent clocking presented by Pavan Bigli during Poster session auto-solves this issue.

## Slide 17: New Clocking
New Clocking
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
No more dip or pixel shifting!

## Slide 18: Possible explanation
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Not symmetric node mapping of the CCD.
Mislabeling of nodes?
    Either on the datasheet or on our camera…
Pinout strictly symmetric but package is oriented.
Barrier Phase
Collecting Phase
Transfer Gate
Transfer Gate
3 Collecting Phases
2 Collecting Phases

## Slide 19: Another transfer issue
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Closer look at the Photon Transfer Curve
VERY subtle dip
Recommended voltage from e2v’s datasheet

## Slide 20: Another transfer issue - autocorrelation
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Autocorrelation of each frame shows excess correlation only in the vertical direction for this exact level.
VERY subtle dip

## Slide 21: Another transfer issue - Fix
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Problem fixed increasing the voltage on the serial register to “help” electrons falling from the transfer gate.
Increase of the serial register’s voltage
Autocorrelation increase with signal is due to Brighter-Fatter effect discussed by Antilogus et al.

## Slide 22: Conclusion
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Exact shape of the electric field over the nodes is complex, especially at the edges.
  1-D representation is simplistic.
We should not assume that a same voltage applied on a node results on a same shape of electric field everywhere. => Keep some margin, increase delta.
0V
10V
Voltage
distance
-5V

## Slide 23: InfraRed Inspection
We do know that the 8 lasts rows of the sensor and the transfer gate aren’t made with the same lithographic mask than the image area.
  Maybe some discrepancies?
Optical microscope with SWIR Camera + narrow IR filter
  Lack of contrast and Magnification
We can’t explore further the CCD itself.
  => Call for help and ideas.
Parallel Phases
Serial register
Image Area
Serial Phases
Zoom : 10x
Pixel size
Transfer Gate
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion

## Slide 24: Surface Full Well
Surface Full Well
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion

## Slide 25: Surface Full Well – On Sky
Long tail forward and backward of an over-illuminated star on the Field of View
  The forward tail is caused by the charges left beyond during the previous frame reading. (persistence)
“LOG” scale
“Histogram” scale
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Even worse than blooming.

## Slide 26: Surface Full Well – Pin Hole setup
A pin hole allows to characterize in lab the levels of both spot and tail.
Blooming Well
or ADC saturation
Surface Well
~340ke-
~510ke-
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Saturation is occurring before the tail appears.
Fake Star
Spot level
Tail level on the overscan
Reference

## Slide 27: Surface Well and Blooming
Surface Well can occur after blooming.
D.P. Weatherill, R. Plackett, K.Arndt and I.P.J. Shipsey
“Modelling charge storage near full well in CCDs”
Journal of Instrumentation. May,17. 2017
SiO2 interface
Blooming
Surface Well
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion

## Slide 28: Surface Full Well – Pin Hole setup
Decrease of the common mode voltage moves charges away from the surface.
Classical detraping fix.
0V to 10V
-5V to 5V
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
0V to 10V
-5V to 5V
No more tails on the brightest stars
Drawback: Increase of the lateral charge diffusion

## Slide 29: Surface Full Well – Optimization
Two successive states:
  Exposure: High common mode voltage to Reduce Lateral Diffusion
  ReadOut: Low common mode voltage to suppress Surface Well
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Surface Well suppressed
Even Steeper PTC !
0V to 10V
-5V to 5V
0V to 10V during Exposure
-5V to 5V during ReadOut
No more tails on the brightest stars
Less lateral diffusion

## Slide 30: Pixel Response Non Uniformity
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
Pixel Response Non Uniformity

## Slide 31: Pixel Response Non Uniformity
Co addition of 15 flats of ~43ke- (Shot noise well below PRNU)
Normalization by a filtered version of itself (To get rid of flat field gradient)
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
9x9 BoxCar filtering
=

## Slide 32: Pixel Response Non Uniformity
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
2 Collecting phases (datasheet standard clocking)
  PRNU = 0.38%
3 Collecting phases
  PRNU = 0.28%

## Slide 33: Pixel Response Non Uniformity
Lithographic mask stitching is visible on high-intensity frames.
Masks of 512x256 pixels
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
12*512=6144 pixels
24*256=6144 pixels
8 extra pixels
E2v-231
6144(H) x 6160 (V)
8 extra pixels
Figure: average on vertical and horizontal directions

## Slide 34: Summary
Benefits of new clocking and new voltages:
  No more strange dip on the PTC. (both pixel shifting and defective line transfer).
  No more catastrophic Surface Well effect on bright objects.
  Improvement of the PSF with high levels (less lateral diffusion or “brighter-fatter” effect).
  Improvement of the PRNU using 3 storage phases instead of two.
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion

## Slide 35
Thank your for your attention.

## Slide 36
Extra Slide: Best setup
Tail level: 2 adu with saturation of about 1.8Me-
0V to 10V
-5V to 5V
0V to 10V during Exposure
-5V to 5V during ReadOut
3V to 13V during Exposure
-8V to 2V during ReadOut

## Slide 37
Extra Slide: Down side
Photon Transfer curve using the new clocking on the down side of the sensor.
Assuming one extra node.
No ”Downing Dip”
-4V to 2V on // clock
0V to 10V on // clock

## Slide 38: Extra Slide: Inverted Clocking
0V
15V
distance
-5V
0V
15V
distance
-10V

## Slide 39: Mechanism: Case 1
TGD | IPHI3 | IPHI2 | IPHI1 | IPHI4 | IPHI3 | IPHI2 | IPHI1
Time
Serial Register
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion
X
X
X
X

## Slide 40: Mechanism: Case 2
TGD | IPHI3 | IPHI2 | IPHI1 | IPHI4 | IPHI3 | IPHI2 | IPHI1
Time
Serial Register
X
Intro | Parallel Transfer | Surface Well | PRNU | Conclusion